The utilization of state-of-the-art graphene derivatives in electrochemical sensor technology for the detection of neonicotinoids

Lueda Kulla1,2

Marina Kuqi1, Petr Jakubec3, David Panáček3,5, Michal Otyepka3,4, Majlinda Vasjari1,2, Besnik Baraj1,2

1 Department of Chemistry, Faculty of Natural Science, University of Tirana, Bulevardi Zogu I, 1001 Tirane, Albania

2Nano-Alb, Academy of Sciences of Albania, Sheshi "Fan Noli", No 7, 1001 and Tirana 
3 Czech Advanced Technology and Research Institute (CATRIN), Regional Centre of Advanced Technologies and Materials, Palacký University Olomouc, Šlechtitelů 27, Olomouc, 77900 Czech Republic

4IT4Innovation, VSB – Technical University of Ostrava, 17. listopadu 2172/15, 708 00 Ostrava-Poruba, Czech Republic

5Nanotechnology Centre, Centre of Energy and Environmental Technologies, VSB – Technical University of Ostrava, 17. listopadu 2172/15, 708 00, Ostrava-Poruba, Czech Republic

kullalueda@gmail.com

Neonicotinoids, widely used herbicides in agriculture, have become a key focus of research due to their potent acute toxicity and neurotoxic effects resulting from prolonged exposure [1]. The main goal of this study is to develop an innovative electrochemical sensing material using state-of-the-art graphene derivates [2][3] for monitoring neonicotinoids level in the environment. To achieve this goal, we selected and evaluated four graphene derivatives—graphene acid (GA), graphene acid with iron nanoparticles (GAFe), nitrogen-doped graphene (GN3) and cyano-graphene (GCN) —as potential candidates for detecting structurally similar pesticides [4,5]. The sensor was characterized using electrochemical impedance spectroscopy (EIS), cyclic voltammetry (CV) and square-wave voltammetry (SWV). The results indicate that these derivatives exhibit improved analytical performance compared to a bare glassy carbon electrode (GCE), which can be attributed to their high conductivity and enhanced electron transfer ability on the electrode surface. Optimization of the square-wave voltammetry technique and pH value was carried out using a factorial design. The GCE/GAFe-based sensor demonstrated a significant electrochemical response to paraquat (PQ), with a sensitivity of 0.07 (μA/mM), correlation of 0.984, and a linear range of 0.05 to 1. 25mM. These findings highlight the potential of graphene-based materials for efficient and sensitive detection of neonicotinoids and structurally related pesticides, such as paraquat, thiamethoxam, and imidacloprid.

References

- F. Laghrib, et al., Materials Science and Engineering: C, 107, (2020), 110349

- D. Chronopoulos et al., Applied Materials Today, 9, (2017), 60-70

- Y. Wu, et al., Journal of The Electrochemical Society, 168, (2021), 126506

- V. Urbanová, et al., Biosensors and Bioelectronics, 89, (2017), 532-537

- P. Trainwatcharanon, et al., RSC advances, 12, (2022), 16079-16092